## Slide 1: Project 65: Quenching and Partitioning of Ti-6Al-4V and Novel Heat Treatments of β-Ti Alloys to Design Microstructures and Properties
Student: Valava Sambandam Rani (Mines)
Faculty: Dr. Amy Clarke (Mines)
Industrial Mentors: ATI, Benjamin Ellyson (LLNL)
Semi-annual Fall Meeting
September 2023

## Slide 2: Project 65: Quenching and Partitioning of Ti-6Al-4V and Novel Heat Treatments of β-Ti Alloys to Design Microstructures and Properties
Student: Valava Sambandam Rani (Mines)
Advisor(s): Amy Clarke (Mines)
Project Duration
PhD: August 2021 to August 2025
Problem: To enhance the mechanical properties of Ti-6Al-4V and novel β-Ti alloys through heat treatments.
Objective: Develop an in-depth understanding about the effect of heat treatments on the microstructures and mechanical properties of Ti-6Al-4V and novel β-Ti alloys, including with additive manufacturing and heat treatments.
Benefit: Novel heat treatments will be designed to tailor microstructures in Ti-6Al-4V and novel β-Ti alloys which in turn would result in improved mechanical properties.
Metrics |  | 
Description | % Complete | Status
1. Literature review and design of heat treatments | 50% | ●
2. Perform heat treatments | 20% | ●
3. Microstructural characterization (HT microstructural evolution) | 25% | ●
4. Tensile and compression testing (Strain-hardening and elongation behavior) | 25% | ●
5. Understanding the microstructure-mechanical properties relationship | 20% | ●
Recent Progress
Performed inter-critical annealing (i.e. near-transus) heat treatments based on the evolved heat treatment matrix
Conducted mechanical and microstructural characterization on the inter-critically annealed Ti-6Al-4V samples to understand the structure-property relationship in the as-quenched samples
Performed heat treatments and subsequent microstructural characterization to determine the partitioning parameters

## Slide 3: Quenching & Partitioning of Ti-6Al-4V
Ti-6Al-4V
  α + β phases, equilibrium β ~10%
  Ms Temperature ~575°C; β-Transus ~1000°C
  Al stabilizes α; V stabilizes β
Quenching and Partitioning
  Inter-critical anneal + water quench results in α + α’ composite
  Aging + air cooling causes decomposition of α’
  Improves work hardening behavior and strength-ductility balance
B. McArthur MS Thesis

## Slide 4: Previous Work – Dilatometry
Phase Fraction of α’ (%) | Inter-critical Annealing Temperature (°C) |  | 
 | Literature Survey | Thermocalc Simulations | Dilatometry Experiments
25 | 850 | 866 | 826
50 | 920 | 933 | 905
75 | 945 | 966 | 952
100 | 1000 | 989 | >1050

## Slide 5: Previous Work – Inter-critical Annealing
Inter-critical Annealing Temperature (°C) | Expected Phase Fraction of α’ (%) | Obtained Phase Fraction of α’ (%)
826 | 25 | ~24
905 | 50 | ~49
952 | 75 | ~70
1100 | 100 | ~100
Variation of α’ after 952°C unexpected
  Inhomogenous furnace temperature and steep β-phase transformation curve
  Exponential fitting of dilatometry data
Successful in varying α’ with heat treatment
826°C
905°C
952°C
1100°C

## Slide 6: Tensile Testing
Inter-critical Annealing Temperature (°C) | Expected Phase Fraction of α’ (%)
As-received | -
826 | 25
905 | 50
952 | 75
1100 | 100
Strain rate = 0.0254 mm/s

## Slide 7: As-received Mill-Annealed Ti-6Al-4V
Grip Section
Gauge Section
β phase fraction = 10.94%
(110)
(200)
(110)
(200)

## Slide 8: Inter-critical Annealing at 826°C for 2h + WQ
Grip Section
Gauge Section
α’ phase fraction ~25%

## Slide 9: Inter-critical Annealing at 905°C for 2h + WQ
Grip Section
Gauge Section
α’ phase fraction ~50%

## Slide 10: Inter-critical Annealing at 952°C for 2h + WQ
Grip Section
Gauge Section
α’ phase fraction ~75%
(110)

## Slide 11: Inter-critical Annealing at 1100°C for 2h + WQ
Grip Section
Gauge Section
α’ phase fraction = 100%
(110)
(200)

## Slide 12: Partitioning Heat Treatment
TESCAN S8252G RAMAN-SEM/FIB
PANanalytical Empyrean X-ray Diffractometer

## Slide 13: Quenching at 952°C
α’ phase fraction ~75%
XRD peak of β-phase was detected
(110)

## Slide 14: Quenching at 952°C + Partitioning at 500°C
  No change in the microstructure
    α’ phase still intact
  XRD peak of β-phase not detected

## Slide 15: Quenching at 952°C + Partitioning at 600°C
  Start of α’-phase decomposition
    Sub-micron scale globules of β-phase
  XRD peak of β-phase evident
    Partial decomposition of α’ into α+β
(110)

## Slide 16: Quenching at 952°C + Partitioning at 700°C
  Decomposition of α’-phase
    Fine lamellae of α+β
  XRD peak of β-phase evident
    Complete decomposition of α’ into fine lamellar α+β
(110)
(200)

## Slide 17: Take-aways
Inter-critical annealing
  UTS increases with α’ phase fraction
  Maximum strain hardening achieved at 50% α’ phase fraction
Partitioning
  α’ decomposition starts at 600°C
  Complete decomposition of α’ after partitioning at 700°C
(110)
(200)
(110)
(110)

## Slide 18: Work Plan and Progress
Chart: 
| Coursework | Literature Survey | Develop Heat Treatment Matrix | Quenching step | Microstructural Characterization | Partitioning Step | Heat Treatments on novel β-Ti alloys | Mechanical Characterization | PhD Thesis
Start Date | 44409 | 44788 | 44788 | 44819 | 44819 | 45017 | 44621 | 45017 | 45658
days complete | 572.85 | 517.5 | 190.8 | 329.6 | 269.4 | 97.6 | 118.8 | 128.2 | 0
days left | 282.15 | 517.5 | 21.2 | 82.4 | 628.6 | 146.4 | 1069.2 | 512.8 | 212

## Slide 19: Challenges and Opportunities
Quantitative microstructural characterization after partitioning
  SEM imaging and XRD analysis only present qualitative evidence for partitioning
  SEM-EDS and EBSD cannot be used to characterize sub-micron scale partitioning
    Potential solution: Use of TEM EDS or APT

## Slide 20: Future Work
Thank you!
Valava Sambandam Rani
valavasambandamrani@mines.edu
Wrought and AM Ti-6Al-4V
  Determine the partitioning parameters for the as-quenched material using simulation tools and heat treatments
  Conduct mechanical characterization on the partitioned samples with desired microstructures
  Understand the structure-property relationship of this alloy after quenching and partitioning
Heat treatments on β-Ti alloys

## Slide 21: References
[1] O. Dumas , B. Hary , G. Martin , F. Sun , C. de Formanoir , F. Prima , S. Godet, Towards work-hardenability of Ti-6Al-4V through a quenching and partitioning approach, MATEC Web of Conferences 321, 11062 (2020)
[2] Charlotte de Formanoir, Guilhem Martin, Frédéric Prima, Sébastien Allain, Thibaut Dessolier, Fan Sun, Solange Vivès, Benjamin Hary, Yves Bréchet, Stéphane Godet, Micromechanical behavior and thermal stability of a dual-phase α+α’ titanium alloy produced by additive manufacturing, Acta Materialia (2018)
[3] Chafino, J.A., Yamanaka, K., Mercier, F., Rivory, P., Balvay, S., Hartmann, D.J., Chiba, A., Fabregue, D., The influence of temperature during water-quench rapid heat treatment on the microstructure, mechanical properties and biocompatibility of Ti -6Al -4V ELI alloy, Journal of the Mechanical Behavior of Biomedical Materials (2019)
[4] Charlotte de Formanoir, Alice Brulard, Solange Vivès, Guilhem Martin, Frédéric Prima, Sébastien Michotte, Edouard Rivière, Adrien Dolimont & Stéphane Godet, A strategy to improve the work-hardening behavior of Ti–6Al–4V parts produced by additive manufacturing, Materials Research Letters, 5:3, 201-208 (2017)
[5] W. Xu, M. Brandt, S. Sun, J. Elambasseril, Q. Liu, K. Latham, K. Xia and M. Qian, Additive manufacturing of strong and ductile Ti–6Al–4V by selective laser melting via in situ martensite decomposition, Acta Materialia, 85, 74–84 (2015)